## Slide 1: Development of the PANDA Forward RICH with an aerogel radiator
Sergey Kononovab on behalf of the PANDA Forward RICH group
a Budker Institute of Nuclear Physics, Novosibirsk, Russia
b Novosibirsk State University, Novosibirsk, Russia
10th International Workshop on Ring Imaging Cherenkov Detectors (RICH2018)
03.August.2018

## Slide 2: Outline
Introduction
PANDA Forward RICH design
Simulation
Mirror samples measurements
Preliminary beam test results
Conclusion

## Slide 3: Quartz vs Aerogel radiators
Difference in Cherenkov angle θc for π and K
Bands – chromatic dispersion in the wavelength range 350-700 nm
n=1.05

## Slide 4: Focusing Aerogel RICH (FARICH)
T.Iijima et al., NIM A548 (2005) 383 A.Yu.Barnyakov et al., NIM A553 (2005) 70
n=1.030 6.0mm
n=1.027 6.3mm
n=1.024 6.7mm
n=1.022 7.0mm
First sample of 4-layer aerogel
3-layer aerogel 115x115x41 mm3
Focusing aerogel improves proximity focusing design by reducing the contribution of radiator thickness into the Cherenkov angle resolution
Multi-layer monolithic aerogels have been being produced by the Boreskov Institute of Catalysis in cooperation with the Budker INP since 2004.
Photon detector
Aerogel
Particle
Cherenkov light
Notes: Идея ФАРИЧ появилась в 2004 г.
Точность измерения черенковского угла связана с точностью измерения скорости, а значит с качеством разделения частиц.

## Slide 5: PANDA detector
Forward RICH
Endcap Disc DIRC
Barrel DIRC
For details of the PANDA experiment see the talk on the PANDA DIRC detectors by J. Schwiening in the Saturday morning session
Antiprotons P=1.5 – 15 GeV/c with
Luminosity up to 2∙1032 cm-2 s-1
Interaction rate up to 2∙107 s-1

## Slide 6: Requirements for the PANDA Forward RICH
Charged PID in the Forward Spectrometer
|θx| < 10°, |θy| < 5°
Approximately 3 x 1 m2 transverse active size, ~0.8 m space occupied along the beam
Working momentum range for 3σ separation
  π /K: 2÷10 GeV/c
  μ/π: 0.5÷2 GeV/c possible may complement the muon system
Physics cases: processes with high charged hadrons multiplicity in the final states for high beam momenta

## Slide 7: PANDA FRICH baseline design
Photon Detector
H12700 MaPMTs (Hamamatsu)
flat panel
8x8 anode pixels of 6mm size
Aerogel radiator
Focusing 2- or 3-layer aerogel
n≈1.05
Total thickness – 40 mm
Mirrors
2 mm float glass
Al+SiO2 coating
DiRICH FEE (GSI)
Designed for H12700 readout
12x32ch preamp+disc+TDC
2 Gbps output link

## Slide 8: Readout candidates for PANDA FRICH
MaPMT Hamamatsu H12700B with DiRICH (GSI) FEE
Digital Photon Counter
Digital silicon photomultiplier
TDC on-chip
a)
b)
Cherenkov spectrum
H12700 QE
DPC3200-22 PDE

## Slide 9: Comparison of photon detector options
MaPMT H12700
(Hamamatsu, Japan)
High active/total area ratio 87%
Robust
Long lifetime
High single photon efficiency
The MaPMT option was chosen for PANDA Forward RICH
Digital Photon Counter
(Philips Digital Photon Counting, Aachen, Germany)
Interesting readout solution – SiPM integrated with ASIC: TDC with 20 ps LSB, able to inhibit individual cells
Immune to magnetic field (not an issue for the PANDA FRICH)
High dark count rate, long dead-time (720 ns) – needs to be cooled for single photon detection
Low measured Npe and PDE – about 2 times lower than expected from the producer’s data
Radiation hardness issues (DPC lifetime would be less than 1 year in the PANDA HL mode)

## Slide 10: MC simulation of the PANDA Forward RICH
FRICH
PANDA Forward Spectrometer geometry in PandaRoot

## Slide 11: Description of inactive material in PandaRoot
Elements to be described
Aerogel+Frame
Mirror+Frame
Photodetector+Frame
Envelope
Current version
only main elements
Full version
in progress

## Slide 12: Simulation code variants
FULL | FAST
Passage of particles through matter | 
Optical processes | -
Digitization | -
Tracking | 
Full event reconstruction | Calibration based event reconstruction
PID | 
Processes described in two simulation variants

## Slide 13: Hit pre-selection
TA, ns
θC, rad
1000 events
Hits around peak in θс-TA are selected for fitting
time in aerogel
hit time

## Slide 14: Ring fitting
Muons
p = 10 GeV/c
β = 0.99994θθ
βFIT = 0.99912
θc , mrad
φc , mrad
Fit dependence by an analytical formulae for each event and obtain particle’s velocity as a result

## Slide 15: Event reconstruction in simulation DPC photon detector
β distribution
distribution
number of hits
event fit

## Slide 16: Focusing aerogel optimization (1)
1.05 − δn
1.05 + δn
1.05 − δn
1.05
1.05 + δn
Two layers
Three layers
Optimize Cherenkov angle resolution by varying

## Slide 17: Focusing aerogel optimization (2) DPC photon detector
Two layers
Optimal values:
mrad
Three layers
mrad
3-layer aerogel was chosen for the following simulation

## Slide 18: MC FRICH PID vs momentum H12700 photon detector
● π
○ K
Reconstruction efficiency
(reconstructed β is within ±3σ of expected)
K identification efficiency at 1% π misidentification
εreg
εK
P, GeV/c
P, GeV/c
● π
○ K
εreg
P, GeV/c
● π
○ K
εreg
P, GeV/c

## Slide 19: MC FRICH PID uniformity H12700 PD, p− beam@ 10 GeV/c
π reco efficiency
K reco efficiency
K identification efficiency at 2% π misidentification
X (cm)
Y (cm)
Y (cm)
X (cm)
X (cm)
Y (cm)
X (cm)
Y (cm)
Y (cm)
X (cm)

## Slide 20: Mirrors for Forward RICH
Float glass + Al + SiO2
Requirements on flatness for float glass (few μm) are met.
Mirror samples from two producers were obtained and compared by reflectivity.
Samples from the Tomsk Institute of High-Current Electronics: Float glass(4mm)+Al+SiO2
Samples from BINP: Glass(2mm)+Al+MgF2

## Slide 21: Mirror reflectance measurements
Chart: Tomsk samples: Al(215nm) + SiO2(130 nm)
130-2 | 0.88 | 0.9
130-4 | 0.89 | 0.87
130-5 | 0.9 | 0.88
130-6 | 0.85 | 0.84
130-7 | 0.89 | 0.89
130-1 with monochromator
with laser
Chart: Tomsk samples: Al(215nm) + SiO2(260 nm)
260-1 | 0.83 | 0.77
260-2 | 0.83 | 0.84
260-3 | 0.9 | 0.87
260-3 with monochromator
with laser
V-W scheme for reflectance measurement
Light source
Monochromator slit
Rotated aux. mirror
Sample position
V
W

## Slide 22: Reflectance vs angle of incidence
Chart: λ = 518 nm
| 68.198591676990731 | 29.981639880280969 | 17.185706437381317 | 11.929322380730632 | 9.6197279637937196
130-5 | 0.83333 | 0.84 | 0.86452 | 0.88387 | 0.88158
260-1 | 0.81046 | 0.79739 | 0.81699 | 0.82468 | 0.83007
312-2 | 0.77143 | 0.80142 | 0.8 | 0.8227 | 0.84173
Chart: λ = 473 nm
| 68.198591676990731 | 29.981639880280969 | 17.185706437381317 | 11.929322380730632 | 9.6197279637937196
130-5 | 0.77901 | 0.86813 | 0.87845 | 0.8674 | 0.8895
260-1 | 0.73437 | 0.85827 | 0.86047 | 0.89062 | 0.87597
312-2 | 0.80663 | 0.86667 | 0.89444 | 0.9011 | 0.90608
collimator
photodiode
mirror
collimator
photodiode
A
B
AoI

## Slide 23: Test beam of F(A)RICH prototype at BINP VEPP-4 (2018)
Electron beam parameters in 2018 | 
Energy range | 3 GeV
Averaged intensity | up to 100 e− / s
Energy spread | 2.6%
Purpose of beam tests for PANDA FRICH:
Test H12700 MaPMTs and PADIWA&TRB3 readout
Obtain single photon resolution for several aerogel configurations and compare with expected ones

## Slide 25: F(A)RICH prototype readout
Custom adapter board to couple 4 PADIWAs to a H12700 MaPMT (PADIWA couple with Planacon MCP PMT without adapter)
2 TRB3 boards and 14 PADIWA3 boards – 224 channels (three and a half MaPMTs)
Each TRB board transmits data via Gbit-ethernet switch to a PC
GSI DABC software used for DAQ from TRB
Triggered by coincidence of signals from the sc. counter before F(A)RICH and the NaI calorimeter
Trigger signal is blocked by PC for readout period. Sync between subsystems is assured by the same event number observed
Custom adapter
TRB3 boards
PADIWA
H12700
Planacon MCP PMT

## Slide 26: Tested aerogel radiator samples (test beam run on 3-4 June 2018)
Configuration 1 n1 = 1.0514, t1 = 2 cm
n2 = 1.0503, t2 = 2 cm
Configuration 2 n1 = 1.0514, t1 = 2 cm
n2 = 1.0514, t2 = 2 cm
2
1
Monolithic aerogels: 3 three-layer samples of 30-40 mm thickness
About 300k event per setup configuration were collected

## Slide 27: Event selection
NaI calorimeter amplitude distribution
and selected interval
Reconstructed track position XY-map at PMT
and selected region

## Slide 28: Hit plots
Hit timing distribution
VEPP-4M bunch structure can be seen with 600 ns separation.
Timing resolution here is determined by the rough measurement of reference timing in TRB3
Hits are selected by leading edge timing in 30ns interval
Hit XY map
Ring is not seen here because the e− beam is wide
Next bunch
Coincident bunch
Trailing edge
Leading edge

## Slide 29: Track adjusted hit position
Preliminary results:
R = 204 mm
σR1 = 4.4 mm (6.6 mrad)
Preliminary
Configuration 1
Aerogel-PMT distance: 600 mm
Background hits are to be understood
Preliminary
PMTs
Aerogel

## Slide 30: Conclusion and outlook
Forward RICH PandaRoot simulation is almost ready.
Mechanical design draft is almost ready.
MaPMTs and FEE tests are in progress. DiRICH electronics is to be tested.
Mirror samples for FRICH were produced. Absolute reflectance measured is close to 85% — satisfactory.
FRICH prototype based on H12700 MaPMTs and PADIWA3+TRB3 with beams was tested in 2018. Data analysis is in progress.
TDR to be ready in 2019