## Slide 1: Cherenkov detectors with aerogel radiators
E.A.Kravchenko
Novosibirsk State University
Budker Institute of Nuclear Physics

## Slide 2
I want to tell a story…
A story about love…
The love between
Prince Cherenkov Light and
Princess Aerogel

## Slide 3: Cherenkov radiation and its main features
The direction of Cherenkov light and intensity both depend on particle velocity
The quadratic dependence of the intensity on charge of the particle
Instantaneous flash, no decay time
Low intensity
Cherenkov photons 100% linear polarized
n
γ
γ
γ
γ
z, v > c/n
Θ
Year of discovery: 1934

## Slide 4: Why we want to use aerogel?
In the range of momenta below 700 MeV/c pions and kaons are identified be means of TOF or dE/dx methods.
To identify pions and kaons above 700 MeV/c it is possible to use Cherenkov threshold counter having (π) = 400--500 МэВ/с => n=1.03-1.06 ! =>
 | n | Pπ, MeV/c | PK, MeV/c
Fused silica | 1.458 | 132 | 465
Water | 1.33 | 159 | 563
Freon 114, 1 atm | 1.0014 | 2640 | 9330
СО2, 1 atm | 1.00043 | 4760 | 16800
СО2, 10 atm | 1.0043 | 1500 | 5320
C2H4, 25 atm | 1.02 | 600 | 2460
AEROGEL

## Slide 5: What it is -- Aerogel?(1)
Aerogel was first synthesized by Samuel Stephens Kistler in 1931
S.S.Kistler, "Coherent Expanded Aerogels and Jellies“, Nature, 1931,vol. 127, p. 741
Aerogel – is a porous material with pore dimension less than visible light wavelength.
It is a classical nanomaterial.The most widespread are silicon dioxide aerogel, although aerogels based on metal oxides, carbon, gelatin and others exist.

## Slide 6: What it is -- Aerogel?(2)
Production method:
Synthesis of the alcogel:
Si(OR)4 + 2H2O => SiO2 + 4HOR
alkoxide water silica alcohol
Supercritical drying in the autoclave to remove alcohol Pmax=100 atm, Tmax= 260°C
  methanol -- Pcr=81 atm, Tcr=230°С
  isopropanol -- Pcr=53 atm, Tcr=235°С
  carbon dioxide -- Pcr=73 atm, Tcr=31°С
Aerogel parameters:
Density 0.003 до 1.0 g/cm3 (fused silica ρ=2.2 g/cm3 )
Refractive index
n ≈ 1 + 0.2·ρ[g/cm3 ] =>
(n = 1.0006 ÷ 1.2)
Porosity up to 99.8%
Inner surface 800 m2/g

## Slide 7: How it all began?
1973
n=1.01—1.06 (1.2 using sintering)
Lsc(400) = 6 mm
There is a Cherenkov light from aerogel!
‘The are no evident signs of scintillations in aerogel’!

## Slide 8: TASSO aerogel threshold Cherenkov detectors
1976- start of the R&D
The first large scale detector with aerogel, 32 detectors, VΣ=2000 l
Large counters 0.35x1.0x1.5 m
n=1.020—1.026
Lsc(400) = 20 mm
Npe = 3.9 (problems with degradation)
H. Burkhardt et.al., NIM184(1981)319
Yes, this is possible!

## Slide 9: KEDR aerogel counters with direct light collection(1)
1982 – SLAC instrumentation conference, talk of Gunter Poelz on TASSO Cherenkov Counters
Start of the R&D at 1986 as part of KEDR project together with Boreskov Institute of Catalysis
1988 – the first aerogel samples produced at BIC
1990 – test of the first prototype on cosmic muons

## Slide 10: KEDR aerogel counters with direct light collection(2)
n=1.035, 10 cm thickness
Lsc(400) = 20 mm
2 Fine Mesh Hamamatsu R2490-01PMTs (working magnetic field 2 T!)
Npe = 6.3 (for β=1 particle)
But! For the whole system 360 Hamamatsu FM PMT are required.

## Slide 11: Era of high transparency aerogel
One-step technology
Direct alcogel synthesis
Si(OR)4 + 2H2O => SiO2 + 4HOR
alkoxide water silica alcohol
Lsc(400) ~ 20 mm
Two-step technology
A mixture of oligomers preparation
SikOl(OR)m(OH)n=>SiO2+alcohol
Lsc(400) > 35 mm
Two-step technology was implemented at BIC in 1992
L.W.Hrubesh, T.M. Tillotson, J.F. Poco “Characterization of ultralow-density silica aerogels
made from a condensed silica precursor”, MRS Proc. 180(1990)315

## Slide 12: Belle aerogel Cherenkov counters
1992 – seminar of A.Onuchin at KEK on aerogel threshold detector development
1994 – approval of KEKB with Aerogel Cherenkov Counters as baseline for PID
Very intensive R&D both on aerogel production and detector design
1124 detectors equipped with 2024 Fine Mesh PMTs (2, 2.5, 3 inch)
n=1.01—1.03, VΣ=2000 l, high transparency hydrophobic aerogel
Npe = 20—26(!)
In operation 1998-2010
Full success of the project!

## Slide 13: Aerogel threshold counters with wavelength shifters(1)
At λ=400 nm
  Lsc~ 40 mm, Labs~ 4-5 m
At λ=300 nm
  Lsc~12 mm, Labs~ 0.5-1 m
  But!
  dN/dλ ~1/λ2
  At ~300 nm Number of Cherenkov photons is 3 times larger than at ~400 nm
  The idea is to absorb Cherenkov photons at short wavelengths and re-emit at large where aerogel transparency is better.

## Slide 14: Aerogel threshold counters with wavelength shifters(2)
Several aerogel detectors used wavelength shifters to increase signal:
The prototype of aerogel Cherenkov detector for BaBar tested PTFE reflector impregnated with PMP dye
AMS-01 Aerogel counters used 25 μm tedlar film soaked in PMP. Suffered a fast degradation Npe = 5 -> 1.5 (n=1.035)
DIRAC uses Teflon foils coated with p-terphenyl. This gave 50% increase of light yield and also increase under threshold efficiency to 40%. (n=1.008, Npe=4)
In these detectors the re-emitted light came back to aerogel and only after that has been collected on the PMT

## Slide 15: ASHIPH detectors
Aerogel SHIfter and PHotomultiplier
Suggested at BINP. A.Onuchin et.al. NIM A315(1992)517
PMMA light guide doped with BBQ dye
is used as wavelength shifter

## Slide 16: KEDR ASHIPH system
160 counters in 2 layers
Solid angle 96% of 4π
n=1.05, VΣ=1000 l, high transparency SAN-96 aerogel
π/K- separation in the momentum range 0.6÷1.5 GeV/с
160 MCP PMTs, photocathode diameter ø18mm, able to work in the magnetic field up to 2 T
Fully installed in the detector in 2013. Now in operation.
-> talk of I.Ovtin

## Slide 17: Ring Imaging Cherenkov detectors with aerogel radiators
If the Cherenkov radiation angle is measured, the precision in the determination (identification) of particle masses will be higher than in threshold counters.
In the 1980s and 1990s, a whole series of RICH detectors were constructed:
CRID, SLD detector, SLAC(C6F14 n=1.277, C5F12/N2 n=1.0017)
RICH, Delphi detector, CERN, (C5F12|C6F14, C4F10)
RICH, CLEOIII detector, Cornell, (LiF, n=1.50)
DIRC, детектор BaBar, SLAC, США (SiO2, n=1.47)
Main problem – they do not provide pion-kaon identification in the range of momenta 4—10 GeV/c
Material with n=1.03-1.05 is needed. Aerogel!
A.Roberts, Nucl. Instrum. and Methods 9(1960)55
J.Seguinot and T.Ypsilantis, Nucl. Instrum. and Methods 142(1977)377

## Slide 18: Peculiarities of aerogel use in RICH detectors
For a long time, it was considered impossible to use aerogels in RICH detectors owing to the strong scattering of light.
1991 – the first experimental observation of Cherenkov ring from aerogel using photography method(A.I.Vorobiov, V.P.Zrelov, J.Ruzichka, “On some peculiarities of Vavilov-Cherenkov radiation in aerogels”, In Frascati 1991, Physics and detectors for DAPHNE, the Frascati Phi-factory* 551-556) (This was `Novosibirsk` aerogel!)
The first RICH with aerogel was proposed D. Fields in 1994
1995 г– Aerogel RICH for LHCb was suggested. The requirement on minimal light scattering length was elaborated. (400 nm) (J.Seguinot, T.Ypsilantis, NIM A368(1995)229)
1995-1996 г. – two-step aerogel production was optimized, =40-50 mm (400 mm) (A.R.Buzykaev et.al, NIM A379(1996)465)

## Slide 19: Why Aerogel?
The difference of Cherenkov angles for different particles is larger
Aerogel refractive index dispersion is smaller
The large number of detected photons from high refractive index radiators can not compensate these effects (~ 1/√Npe)

## Slide 20: The first aerogel RICH
Hermes RICH (DESY, Германия)
Matsushita aerogel, n=1.03
Start of the design – 1996
Start of the operation -- 1998

## Slide 21: Aerogel in LHCb RICH1
LHCb RICH1 (CERN, Швейцария)
BIC/BINP production, n=1.03, 20x20x5 cm tiles
Aerogel did not work. – small number of photoelectrons in the ring + strong pile-up noise

## Slide 22: Aerogel RICH at AMS-02 at ISS
Measurement of Z of the nucleon, Npe~Z2
BIC/BINP production, n=1.05
-> the talk of F. Giovacchini

## Slide 23: Further progress – Focusing aerogel RICH!
Suggested in 2004
T.Iijima et al., NIM A548 (2005) 383 A.Yu.Barnyakov et al., NIM A553 (2005) 70
2017

## Slide 24: Aerogel RICH for CLAS12
-> Talks of Marco Mirazita and Marco Contalbrigo

## Slide 25
This is not the end of the story..
Princess Aerogel and Prince
Cherenkov Light are still young
and love each other,
they have a lot of children
and planning to have more…
Thank you!

## Slide 26: Additional slides

## Slide 27: ASHIPH long term stability
A prototype of the endcap ASHIPH counter are under operation since 2000. From time to time it is tested in Cosmic Ray Telescope (CRT). Its signal degradation now has stabilized at the level of 60% from initial value.

## Slide 28: Detectors with record timing resolution
The task:
Measurement of the longitudinal profile of particle beam
Transition radiation used usually.
Advantages of Cherernkov radiation:
  Higher intensity
  Directionality
 | n=1.01 | n=1.03 | n=1.05 | n=1.01
h, mm | 20 | 2 | 1 | 1
RMS, пс | 0.58 | 0.110 | 0.091 | 0.017
J.Bahr, A.Onuchin et.al., NIM A538(2005)597

## Slide 29: Aerogel sample
100x100x31 mm3
Lsc(400nm)=43 mm
n2=1+0.438*ρ
 | n | h, mm
Layer 1 | 1.050 | 6.2
Layer 2 | 1.041 | 7.0
Layer 3 | 1.035 | 7.7
Layer 4 | 1.030 | 9.7
 | n | h, mm
Layer 1 | 1.050 | 6.2
Layer 2 | 1.041 | 7.0
Layer 3 | 1.035 | 7.7
Layer 4 | 1.030 | 9.7

## Slide 30: Разработка аэрогеля для Черенковских счетчиков в Новосибирске
n = 1.006 – 1.06 (1.13)
Aerogel development has started in 1986 (KEDR detector project)
More than 3000 liters have been produced:
2000 liters – KEDR and SND ASHIPH counters
~ 1 м2 LHCb RICH,
~ 2 м2 AMS02 RICH
~ 5 м2 CLAS12 RICH

## Slide 31: Aerogel degradation due to water adsorption(1)
Aerogel internal surface is 106 times greater than external. Adsorption of water is very fast process (1-10 hours).
Degradation of the light absorption length is very slow process (1-2 months) after water absorption.
The time and the level of the degradation are depend on the impurities in aerogel from raw materials and production procedure (Fe, Mn, Cr, etc.).
Concentration of metals in aerogel, ppb |  |  |  | 
Fe | Cu | Mn | Cr | Ni
500 | 56 | 7 | 26 | 

## Slide 32: Aerogel degradation due to water adsorption(2)
The refractive index (n-1) and light scattering length depends on amount of adsorbed water and are changed less than 10% after water adsorption of 2-4% of aerogel mass.
The light absorption length (Labs) in different aerogel samples after baking is the same, but after water impregnation could be very different
It is possible to make aerogel selection after water impregnation
One atom Fe is able to attract 6 molecules of water
To achieve maximum degradation of Labs it is enough to adsorb 1ppm of water.
(NIM A598 (2009) 166-168)

## Slide 33: KEDR ASHIPH system(2)
Npe = 6.4±0.2 – layer 1
Npe = 5.0±0.2 – layer 2
Npe = 10.9±0.2 – sum of the signals in 2 layers (80%)
π/K separation at 1.2GeV/c is 4.3σ
-> talk of I.Ovtin